## Slide 1: 2d photonic crystals
Steven G. Johnson, MIT
18.369/8.315, Spring 2018
See also chapters 5 and 10 of Photonic Crystals: Molding the Flow of Light

## Slide 2: 2d periodicity, ε=12:1
E
H
TM
a
Frequency ω (2πc/a) = a / λ
Γ
X
M
Γ
X
M
Γ
irreducible Brillouin zone
gap for
n > ~1.75:1
k

## Slide 3: 2d periodicity, ε=12:1
E
H
TM
Ez
–
+
Ez
(+ 90° rotated version)
gap for
n > ~1.75:1
Γ
X
M
Γ

## Slide 4: 2d periodicity, ε=12:1
E
H
E
H
TM
TE
a
frequency ω (2πc/a) = a / λ
Γ
X
M
irreducible Brillouin zone
Γ
X
M
Γ
k

## Slide 5: What a difference a boundary condition makes…
ε1
ε2
E1,|| = E2,||
ε1E1,⊥ = ε2E2,⊥
E|| is continuous:
energy density ε|E|2
more in larger ε
εE⊥ is continuous:
energy density |εE|2/ε
more in smaller ε
To get strong confinement & gaps,
want E mostly parallel to interfaces
TM: ||
TE: ⊥

## Slide 6: 2d photonic crystal: TE gap, ε=12:1
TE bands
TM bands
gap for n > ~1.4:1
E
H
TE

## Slide 7: “Complete” (TE+TM) gap in 2d
Spots: big enough for lowest TM bands
to concentrate (gap with 3rd band)
Veins: lowest TE band circles around holes

## Slide 8: 3d photonic crystal: complete gap , ε=12:1
I.
II.
[ S. G. Johnson et al., Appl. Phys. Lett. 77, 3490 (2000) ]
gap for n > ~2:1

## Slide 9: Intentional “defects” are good
microcavities
waveguides (“wires”)

## Slide 10: Resonance
420 nm
[ Notomi et al. (2005). ]
an oscillating mode trapped for a long time in some volume
(of light, sound, …)
frequency ω0
lifetime τ >> 2π/ω0
quality factor Q = ω0τ/2
energy ~ e–ω0t/Q
modal
volume V
[ Schliesser et al.,
PRL 97, 243905 (2006) ]
[ Eichenfield et al. Nature Photonics 1, 416 (2007) ]
[ C.-W. Wong,
APL 84, 1242 (2004). ]

## Slide 11: Why Resonance?
an oscillating mode trapped for a long time in some volume
• long time = narrow bandwidth … filters (WDM, etc.)
— 1/Q = fractional bandwidth
• resonant processes allow one to “impedance match”
hard-to-couple inputs/outputs
• long time, small V … enhanced wave/matter interaction
— lasers, nonlinear optics, opto-mechanical coupling,
sensors, LEDs, thermal sources, …

## Slide 12: How Resonance?
need mechanism to trap light for long time
[ llnl.gov ]
metallic cavities:
good for microwave,
dissipative for infrared
ring/disc/sphere resonators:
a waveguide bent in circle,
bending loss ~ exp(–radius)
[ Xu & Lipson
(2005) ]
10µm
[ Akahane, Nature 425, 944 (2003) ]
photonic bandgaps
(complete or partial
+ index-guiding)
VCSEL
[fotonik.dtu.dk]
(planar Si slab)

## Slide 13: Why do defects in crystals trap resonant modes? What do the modes look like?

## Slide 14: Single-Mode Cavity
Γ
X
M
Γ
Γ
X
M
frequency (c/a)
Bulk Crystal Band Diagram
A point defect
can push up
a single mode
from the band edge
(k not conserved)

## Slide 15: “Single”-Mode Cavity
G
X
M
G
Γ
X
M
frequency (c/a)
Bulk Crystal Band Diagram
A point defect
can pull down
a “single” mode
(k not conserved)
X
…here, doubly-degenerate
(two states at same ω)

## Slide 16: Tunable Cavity Modes
Ez:
frequency (c/a)
monopole
dipole

## Slide 17: Tunable Cavity Modes
Ez:
band #1 at M
band #2 at X’s
multiply by exponential decay
monopole
dipole

## Slide 18: More defect modes (4 out of 5 C4v irreps here)

## Slide 19: Intentional “defects” are good
microcavities
waveguides (“wires”)

## Slide 20: Projected Band Diagrams
conserved k!
1d periodicity
Γ
X
M
conserved
not conserved
So, plot ω vs. kx only…project Brillouin zone onto Γ–X:
gives continuum of bulk states + discrete guided band(s)

## Slide 21: Air-waveguide Band Diagram
any state in the gap cannot couple to bulk crystal ⇒ localized
continuum of
bulk-crystal modes

## Slide 22: (Waveguides don’t really need a complete gap)
Fabry-Perot waveguide:
This is exploited e.g. for photonic-crystal fibers…

## Slide 23: Guiding Light in Air!
mechanism is gap only
vs. standard optical fiber:
“total internal reflection”
— requires higher-index core
no hollow core!
hollow = lower absorption, lower nonlinearities, higher power

## Slide 24: Review: Why no scattering?
forbidden by gap
(except for finite-crystal tunneling)
forbidden by Bloch
(k conserved)

## Slide 25: Benefits of a complete gap…
broken symmetry –> reflections only
effectively one-dimensional

## Slide 26: Band diagrams: Poor tool to understand refraction/reflection at interfaces
[ M. Notomi, PRB 62, 10696 (2000). ]
Frequency ω (2πc/a) = a / λ
Γ
X
M
Γ
At an interface, only ω and surface-parallel k are conserved.
— we need all the solutions at a given ω, not the different ω’s at a given k.

## Slide 27: “1d” Waveguides + Cavities = Devices
resonant filters
high-transmission
sharp bends
waveguide splitters
channel-drop filters

## Slide 28: Refraction and wavevector diagrams
ω contours
in (kx,ky) space
[ Luo et al, PRB 65, 2001104 (2002). ]
k|| is conserved

## Slide 29: Negative-refractive all-dielectric photonic crystals
[ M. Notomi, PRB 62, 10696 (2000). ]
negative refraction
focussing
(2d rods in air, TE)
not metamaterials: wavelength ~ a,
no homogeneous material can reproduce all behaviors

## Slide 30: “Superlensing” with Photonic Crystals
[ Luo et al, PRB 68, 045115 (2003). ]
2/3 diffraction limit

## Slide 31: Supercollimation
A Gaussian (etc.) beam propagating in the x direction consists of many ky components at the same ω. In a homogeneous medium, each ky component travels in a different direction (group velocity). The beam therefore spreads (diffracts).
In a photonic crystal, the ω contour can be very “flat” so beam spreading is minimized: all the ky components travel in almost the same direction. Supercollimation!

## Slide 32: Supercollimation on the computer:
the light forms one or more coherent “Bloch beams”
that propagate without scattering
… and almost without diffraction (supercollimation)

## Slide 33: Experimental supercollimation
Rakich et al., “Achieving centimetre-scale supercollimation in a large-area two-dimensional photonic crystal,” Nature Materials 5, 93–96 (2006).

## Slide 34: Experimental supercollimation at λ≈1.5µm
Rakich et al., “Achieving centimetre-scale supercollimation in a large-area two-dimensional photonic crystal,” Nature Materials 5, 93–96 (2006).
Theory:
Experiment
(measured
vertical scattering
from disorder)
Theory, including
disorder: