## Slide 1: 2d periodicity, ε=12:1
E
H
TM
a
frequency ω (2πc/a) = a / λ
Γ
X
M
Γ
X
M
Γ
irreducible Brillouin zone
gap for
n > ~1.75:1
k

## Slide 2: 2d periodicity, ε=12:1
E
H
TM
Ez
–
+
Ez
(+ 90° rotated version)
gap for
n > ~1.75:1
Γ
X
M
Γ
min–max theorem: 1st band “wants” to concentrate in high ε, higher bands forced out by orthogonality

## Slide 3: 2d periodicity, ε=12:1: TM gap, no TE gap
E
H
E
H
TM
TE
a
frequency ω (2πc/a) = a / λ
Γ
X
M
irreducible Brillouin zone
Γ
X
M
Γ
k

## Slide 4: What a difference a boundary condition makes…
ε1
ε2
E1,|| = E2,||
ε1E1,⊥ = ε2E2,⊥
E|| is continuous:
energy density ε|E|2
more in larger ε
εE⊥ is continuous:
energy density |εE|2/ε
more in smaller ε
To get strong confinement & gaps,
want E mostly parallel to interfaces
TM: ||
TE: ⊥
is finite, so Ey continuous
x
y
εEx continuous
(since no discontinuity in x)

## Slide 5: 2d photonic crystal: TE gap, ε=12:1
TE bands
TM bands
gap for n > ~1.4:1
E
H
TE
1st Brillouin zone
+ irreducible B.Z.
triangular / hexagonal lattice of air holes in ε=12
Origin of TE gap: 1st band’s
TE (Ex,Ey) electric field lines
can “loop around” cylinders
K
K
M
(C6v)
(C3v)
(C6v symmetry of hexagon)

## Slide 6: “Complete” overlapping TE+TM gap
TE gap: 1st band loops around veins, 2nd band forced out by orthogonality.
TM gap: 1st two bands concentrated in interstitial “spots,” 3rd band forced out by orthogonality.
(In 2d, however, we can generally choose one polarization to work with, so an overlapping TE+TM gap is rarely needed. In 3d, though, modes are no longer purely polarized and we will have to handle every field orientation simultaneously.)
TE+TM

## Slide 7: Brillouin zones: A better unit cell in k
hexagonal / “triangular” Bravais lattice
Reciprocal lattice
• Problem: obvious “primitive cell” in k space breaks C6v symmetry.
primitive
cell?
• Solution: define “first Brillouin zone” as points closer to k=0
than to any other reciprocal lattice vector G.
first Brillouin zone
gives square B.Z.
in square lattice:
(also called “Wigner–Seitz cell” of Bravais lattice,
or “Voronoi cell for any set of points.)

## Slide 8: Single-Mode Cavity “point” defect: break all translation symmetry = localized modes in gap
Γ
X
M
Γ
Γ
X
M
frequency (c/a)
Bulk Crystal Band Diagram
A point defect
can push up
a single mode
from the band edge
(k not conserved)
reduced radius ~ reduced ε
~ higher ω
recall Taylor expansion around M
= analytic continuation in gap: k = M + i(decay)
(this is a cartoon:
k is not conserved)

## Slide 9: “Single”-Mode Cavity
G
X
M
G
Γ
X
M
frequency (c/a)
Bulk Crystal Band Diagram
A point defect
can pull down
a “single” mode
(k not conserved)
rotation of X = Y
…here, doubly-degenerate
(two states at same ω)

## Slide 10: Tunable Cavity Modes
Ez:
frequency (c/a)
monopole
dipole

## Slide 11: Tunable Cavity Modes
Ez:
band #1 at M
band #2 at X’s
≈ multiply by exponential decay
monopole
dipole
from X
from Y
from M

## Slide 12: Other defects = other C4v irreps
 | E | 2C₄ | C₂ | 2σ | 2σ′
Γ₁ | 1 | 1 | 1 | 1 | 1
Γ₂ | 1 | 1 | 1 | -1 | -1
Γ₃ | 1 | -1 | 1 | 1 | -1
Γ₄ | 1 | -1 | 1 | -1 | 1
Γ₅ | 2 | 0 | -2 | 0 | 0
Γ1
Γ4
Γ3
Γ5
(doubly
degenerate)

## Slide 13: Intentional “defects” are good
microcavities
waveguides (“wires”)

## Slide 14: Projected Band Diagrams
conserved k!
1d periodicity
Γ
X
M
conserved
not conserved
So, plot ω vs. kx only…project Brillouin zone onto Γ–X:
gives continuum of bulk states + discrete guided band(s)

## Slide 15: Air-waveguide Band Diagram
any state in the gap cannot couple to bulk crystal ⇒ localized
continuum of
bulk-crystal modes

## Slide 16: Projected band diagram: kx conserved
Γ
X
M
Y
plot all bands vs. kx
gap
Γ
X
X
M

## Slide 17: (Waveguides don’t really need a complete gap)
Fabry-Perot waveguide:
This is exploited e.g. for photonic-crystal fibers…

## Slide 18: Guiding Light in Air!
mechanism is gap only
vs. standard optical fiber:
“total internal reflection”
— requires higher-index core
no hollow core!
hollow = lower absorption, lower nonlinearities, higher power

## Slide 19: Review: Why no scattering?
forbidden by gap
(except for finite-crystal tunneling)
forbidden by Bloch
(k conserved)

## Slide 20: Benefits of a complete gap…
broken symmetry –> reflections only
effectively one-dimensional

## Slide 21: “1d” Waveguides + Cavities = Devices
resonant filters
high-transmission
sharp bends
waveguide splitters
channel-drop filters

## Slide 22: Surface states in 2d
Projected band diagram: only k|| conserved: Plot projected crystal bands + light cone.
Surface termination determines surface state solution: see effect of 2 different terminations!